THE MECHANICAL PROPERTIES OF MATERIALS:

- ELASTIC

  - The ability of a material to "spring back" to its original shape if distorted into some other shape

  - Most solid materials exhibit elastic behaviour, but only if the deformation is not too large.

  - Some materials that exhibit elastic behaviour:

    - Rubber (large deformations if warm, then fracture)

    - Rubber (small deformations if cold, then fracture)

    - Metals (small deformation, then permanently deform)

    - Ceramics (small deformation, then fracture)

    - Electronic materials (small deformation, then fracture or deform)

    - Glass (small deformation, then fracture)

    - Silly putty (large deformations, but only if deformed very rapidly)

    - Human skin (large deformations)

    - Polymers (temperature dependent)

- PLASTIC

- When a material gets stretched or squashed or bent and it stays in its new shape – this happens to some elastic materials when they get bent or stretched too much – the other materials break

- STIFF OR SOFT

- A material that takes a lot of force to stretch or bend in an elastic way is said to be ‘stiff’, a material that takes little force is said to be ‘soft’

- STRONG OR WEAK

- A material that takes a lot of force to stretch or bend in a plastic way is said to be ‘strong’, a material that takes little force is said to be ‘weak’

- BRITTLENESS OR TOUGHNESS

- A material that can bend or stretch a long way before it breaks is said to be ‘tough’, a material that can only bend or stretch a little way is said to be ‘brittle’

THE 4 CLASSES OF MATERIAL:

## METALS

- Distinguishing features

  - Atoms arranged in a regular repeating structure (crystal)

  - Relatively strong

  - Dense

  - Malleable or ductile: high plasticity

  - Resistant to fracture: tough

  - Excellent conductors of electricity and heat

  - Opaque to visible light

  - Shiny appearance

## CERAMICS

- Distinguishing features

  - Most have a regular arrangement of atoms (exception: glasses)

  - Composed of a mixture of metal and nonmetal atoms

  - Lower density than most metals

  - Stronger than metals

  - Low resistance to fracture: low toughness or brittle

  - Low ductility or malleability: low plasticity

  - High melting point

  - Poor conductors of electricity and heat

  - Single crystals are transparent

## POLYMERS

- Distinguishing features

  - Composed primarily of C and H (hydrocarbons)

  - Low melting temperature

  - Some are crystals, many are not

  - Most are poor conductors of electricity and heat

  - Many have high plasticity

  - A few have good elasticity

  - Some are transparent, some are opaque

## COMPOSITES

- Distinguishing features

  - Composed of two or more different materials (e.g., metal/ceramic, polymer/polymer, etc.)

  - Properties depend on amount and distribution of each type of material

  - Collective set of properties more desirable than possible with any individual material

- Applications

  - Sports equipment (golf club shafts, tennis rackets, bicycle frames)

  - Aerospace materials

  - Thermal insulation

  - Concrete

  - "Smart" materials (sensing and responding)

  - Brake materials

- Examples

  - Fiberglass (glass fibers in a polymer)

  - Space shuttle heat shields (interwoven ceramic fibers)

  - Paints (ceramic particles in latex)

  - Tank armor (ceramic particles in metal)